SECTION 09253-CEMENTITIOUS ENCLOSURE - LEAD-BASED PAINT

PART 1 - GENERAL

1.1	RELATED DOCUMENTS

A.	Drawings and general provisions of the Contract,

including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2	SUMMARY

A.	This Section includes the enclosure of lead-based paint

by the following methods:

1.	Cementitious enclosure mechanically attached

directly over lead-based painted surface, on drywall, wood, stucco, plaster and other masonry products.

B.	Related Sections:  The following sections contain

requirements that relate to this section:

1.	Section 01505 - Exterior Regulated areas

2.	Section 01506 - Work area containment

3.	Section 01555 - Worker protection

4.	Section 01556 - Respiratory protection

5.	Section 09953 - Surface preparation - Paint

Stabilization

1.3	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original packages, containers or

rolls bearing brand name and identification of manufacturer or supplier.

B.	Store materials inside under cover and keep dry and

protected against damage from weather, construction traffic and other causes.

1.4	PROJECT CONDITIONS

A.	Environmental conditions, General:  Establish and

maintain environmental conditions for applying and finishing cementitious enclosure according to manufacturers recommendations.

B.	Room temperature:  For adhesive attachment and

finishing of cementitious materials, maintain not less than 40 degrees F (4 degrees C) for 48 hours prior to application and continuously after until dry.  Do not exceed 95 degrees F (35 degrees C) when using temporary heat sources.

C.	Ventilation:  Ventilate building spaces, as required,

for drying cementitious materials.

1.5	SUBMITTALS

A.	Submit copies of manufacturer's specifications, product

data and installation instructions.

B.	Submit Material Safety Data Sheets.

C.	Submit copies of ASTM test results.

PART 2 - PRODUCTS

2.1	MANUFACTURERS

A.	Available manufacturers:  Subject to compliance with

requirements, manufacturers offering products that may be incorporated in the work include, but are not limited to the following:

B.	Subject to compliance with requirements, provide

cementitious enclosure and related products by one of the following:

2.2	CEMENTITIOUS ENCLOSURE SYSTEM MATERIALS

A.	Hard surfaced polymer acrylic cementitious coating

B.	Glass fiber reenforcing mesh

C.	Bonding coating

2.3	MIXING

A.	Mechanically mix cementitious materials to comply with

referenced application standard and with recommendations of manufacturer.

PART 3 - EXECUTION

3.1	GENERAL

A.	Before starting  work of this section, complete the

following:

1.      Section 01506 - Work area containment

2.      Section 01555 - Worker protection

3.      Section 01556 - Respiratory protection

3.2	EXAMINATION

A.	Examine substrates for compliance with requirements for

substrates, installation tolerances, and other conditions affecting performance of  enclosure.  Do not proceed with installation until unsatisfactory conditions have been corrected.

3.3	PREPARATION

A.	Prior to installation of cementitious enclosure

carefully remove flaking and loose areas of lead-based paint in accordance with Section 09953 - Surface Preparation-Paint Stabilization.

B.	Clean substrates of projections and substances

detrimental to application conduct final preparation of surfaces in accordance with manufacturer's written instructions.

C.	Protect adjacent surfaces not to be enclosed.

Immediately remove cementitious material by wet wiping from any surface not intended to be covered.

3.4	APPLICATION

A.	Prepare monolithic surfaces for bonded base coats and

use bonding compound or agent to comply with requirements of referenced plaster application standards for conditioning of monolithic surfaces.

B.	Tolerances: Do not deviate more than 1/8 inch (3.2 mm)

in 10'0" (3.05 m) from a true plane in finished plaster surfaces, as measured by a 10'0" (3.05 m) straightedge at any location on surface.

C.	Apply thickness and number of coats of cementitious

materials required by manufacturer's written instructions.

3.5	WALL APPLICATION

A.	Apply light coat of cementitious material to wall with

a trowel

B.	Trowel reinforcing mesh into the wet base coat.  work

from center to edges.  Embed mesh until uniformly covered and barely visible.

C.	Mechanical fasteners may be installed immediately after

installation of mesh or after curing.  Space fasteners 10" to 24" (25 to 610 mm) o.c.  Drive fasteners into framing or other supports.

D.	Allow base coat to cure in accordance with

manufacturer's written instructions.

E.	Apply finish coat 1/8" to 3/16" (3.2 to 4.8 mm) in

thickness over entire base coat.  Maintain uniform appearance.

3.6	CEILING APPLICATION

A.	Apply bonding agent to ceiling in accordance with

manufacturer's written instructions.  Allow agent to cure completely.

B.	Follow installation instructions for walls above.

3.7	CLEANING AND PROTECTION

A.	Remove temporary protection.  Promptly remove

cementitious material and bonding agent from door frames, windows, and other surfaces that are not to be

enclosed.  Repair floors, walls, and other surfaces that have been stained, marred, or otherwise damaged during the enclosure work.  When work is completed, removed unused materials, containers, and equipment and clean floors of plaster debris.

B.	Provide final protection and maintain conditions, in a

manner suitable to Installer that ensure cementitious enclose work's being without damage or deterioration at time of  Substantial Completion.

END OF SECTION 09253