SECTION 09940 - ENCAPSULATION - LEAD-BASED PAINT

PART 1 - GENERAL

1.1	RELATED DOCUMENTS:

A.	Drawings and general provisions of the Contract, including General and Supplementary Conditions and other Division-1 Specification sections, apply to work of this section.

1.2	SUMMARY OF WORK:

A.	Work under this section includes the furnishing of all labor, materials, and equipment required to encapsulate the following lead-based painted surfaces:

1.	Lead-based painted plaster kitchen walls where cabinetry is located.

2.	Lead-based painted wood crown molding.

1.3	SUBMITTALS:

A.	Before Start of Work:  Submit the following to the Designer for review.  Do not start work until these submittals are returned with Designer action stamp indicating that the submittal is returned for unrestricted use.

B.	Product Data:  Submit product data, use instructions, and recommendations from manufacturer's intended for use.  Include data substantiating that material complies with requirements of this section and the physical properties requirements established by the Commonwealth of Massachusetts.  Submit manufacturer's warranties on the durability of the product.  Provide material safety data sheets.

1.4	DELIVERY AND STORAGE

A.	Deliver materials to the job site in original, new and unopened packages and containers bearing manufacturer's name and label and following information:

Name And Title Of Material

Manufacturer's Name

Manufacturer's Stock Number And Date of Manufacture

Applications Instructions

1.5	JOB CONDITIONS

A.	Apply Encapsulating Materials only when environmental conditions in the work area are as required by the manufacturer's instructions.

1.6	QUALITY ASSURANCE

A.	Installation of encapsulation materials by a firm and personnel approved by manufacturer of the primary encapsulation material.

B.	Testing: Test Encapsulation Material using methods set forth in the HUD guideline until ASTM standard is approved. Test each encapsulant system on each component and surface to receive treatment.  Allow product to cure properly before performance patch test.

1.	X-cut Or Patch Edge Method: Apply encapsulation system in accordance with manufacturer's instructions including adequate cure time before testing.  If inspector can lift, peel or tear a large (1/2 inch x 1/2 inch (13 x 13 mm) or larger square) section of the patch away from the existing top coat then the encapsulant fails the patch test.  For the "patch-edge" method, if the encapsulant can be lifted easily, then the patch test fails.

2.	Soundness Method: Apply encapsulant in accordance with manufacturer's instructions.  When peeled away the paper backing on the wallboard attached to the painted surface should remain.  If the adhesive is removed from the painted surface or if the lead-based paint film splits the test fails.

C.	Performance Warranty:  submit written performance warranty, executed by the manufacturer and co-signed by the contractor, agreeing to repair/replace work that has cracked, peeled, blistered or otherwise deteriorated to a condition where it would not perform effectively for its intended purpose due substantially to defective materials or workmanship, and not due to abuse by occupants.  Improper maintenance, unforeseeable ambient exposures or other causes beyond anticipated conditions and manufacturer's/contractor's control are not covered by the warranty.

1.	Warranty Period is _______ years after date of substantial completion.

PART 2 - PRODUCTS

2.1	ENCAPSULATION SYSTEMS:

A.	Liquid Spreadable Encapsulants

1.	Provide encapsulation system consisting of a durable coating which is compatible with the lead-based painted surface.

a.	Elastomeric

b.	Semi-Rigid, flexible

c.	Rigid

2.	Available Manufacturer's include but are not limited to:

B.	Liquid Spreadable Reinforced Encapsulants

1.	Provide encapsulation system consisting of a coated reinforced covering.

a.	Elastomeric

b.	Urethane/Epoxy

c.	Cementitious

2.	Available Manufacturer's: include but are not limited to:

PART 3 - EXECUTION

3.1	BEFORE STARTING WORK OF THIS SECTION, COMPLETE THE FOLLOWING:

A.	Section 01505 - Exterior Regulated Areas - Lead-Based Paint

B.	Section 01506 - Work Area Containment - Lead-Based Paint

C.	Section 01555 - Worker Protection - Lead-Based Paint

D.	Section 01556 - Respiratory Protection - Lead-Based Paint

E.	Section 09953 - Surface Preparation - Paint Stabilization - Lead-Based Paint

3.2	SURFACE PREPARATION:

A.	Prior to installation of encapsulation system carefully remove flaking and loose areas of lead based paint by wet scraping until a sound, intact edge is achieved.  Remove loose or unsound substrates and repair/replace prior to encapsulation  Paint with good adhesion is to remain.  Follow manufacturer's printed instructions.

B.	Degrease and degloss walls if required by manufacturer's printed instructions.

3.3	ENCAPSULATION APPLICATION:

A.	Apply encapsulation system in accordance with manufacturer's recommendations.  Examine existing conditions to determine surface preparation required and compatibility with substrate.

B.	Encapsulation system shall be applied to the substrate in a continuous system to seal the entire surface being coated.  Number of coats and coverage rates shall be in accordance with manufacturer's recommendations.

C.	Test the adhesion of the system by using minimum 6" X 6" (152 x 152 mm) area in accordance with HUD Guidelines.   The area must pass a visual inspection before applying and performing the patch test to ensure a clean surface and before completing the encapsulation process.

D.	At completion of encapsulation comply with requirements of section 01715 - Project Decontamination - Lead-Based Paint.

E.	At completion of work submit manufacturer's warranty executed by both manufacturer and contractor.

END OF SECTION 09940